## Slide 1: Calculation of saturated coupling loss in Rutherford cables
CHATS 2021
September 21
N. Bykovskiy
D. Uglietti
P. Bruzzone
K. Sedlak

## Slide 2: Outline
Introduction
  Motivation
Saturated coupling loss
  Analytical calculation
  Network modelling
DEMO CS case study
Outlook on network modelling
Conclusion

## Slide 3: Introduction
Large AC losses should then be properly evaluated and accounted in the design. Impact of twisting stacks was found marginal for soldered stacks in fusion conductors, while transposing stacks (twisted or not) have a moderate effect, see https://doi.org/10.1016/j.cryogenics.2020.103118
Development of network models for Rutherford cables:
70’s, Morgan et al: crossing strand coupling, weak excitation, analytical results
80’s, Sytnikov et al: crossing and adjacent, weak and strong, analytical
90’s, Verweij et al: complete numerical electromagnetic model
00’s – p.t.: CUDI / JackPot / THEA / THELMA multi-physics modelling tools
LTS have low stability (low MQE), thus must be operated in weak excitation (coupling currents << Ic), therefore leading to small filaments and short twist-pitches.
In contrast, HTS materials have high stability and could be operated in a strong excitation mode (coupling currents ~ Ic). No need for fine twisted filaments, for example Bi2223 tapes with non-twisted filaments, ReBCO monofilamentary tapes.
response to constant

## Slide 4: Motivation
Strong excitation mode features interplay between coupling current loops and superconducting loops, i.e. corresponding loss contributions are no longer independent.
Furthermore, effects of saturation and screening are counteracting.
Hence, detailed study on the actual AC loss performance is needed.
ASTRA conductor concept for DEMO CS coils operated up to 18 T at 5 K, ≳0.1 T/s transients:
Aligned Stacks Transposed in Roebel Arrangement
Jacket pre-compression
Separate cooling channel (conduction cooled stacks)
Impregnation of cable space

## Slide 5: Analytical calculation: weak excitation
https://doi.org/10.1016/0011-2275(89)90207-5
increases with decreases with :
Limit of the model applicability in terms of the cable twist-pitch?
(e.g. missing geometry factor)
: inter-strand loss
Geometry: slab (see Wilson’s book, section 8.3.1)
Geometry: Rutherford cable

## Slide 6: Analytical calculation: strong excitation
: saturated loss
Perpendicular field (2 layers):
Parallel field (N/2 layers):
(min )
Critical-state model ():
  in perp field
  in parr field
or simply
(perp)
(parr)
Generally, higher loss for finite n-value and same Ic:
for in perp field

## Slide 7: Network modelling: integral formulation
text
Model parameters |  |  | 
Category | Symbol | Description | Value
Geometry |  | Number of strands | 4 – 40
 |  | Strand width | 8 mm
 |  | Strand height | 4 mm
 |  | Cable twist-pitch | 0.1 m – inf
Electrical properties |  | Trans. specific resistance | 1 – 100 µΩ.m
 |  | Critical current | (strand props)
 |  | Index of transition | 1 – 1000
Operating conditions |  | Ramp rate of external magnetic field | 0.01 – 1 T/s
 |  | Field orientation | 0 – 90 deg
 |  | Operating current | 0 to Ic
Model parameters |  |  | 
Category | Symbol | Description | Value
Geometry |  | Number of strands | 4 – 40
 |  | Strand width | 8 mm
 |  | Strand height | 4 mm
 |  | Cable twist-pitch | 0.1 m – inf
Electrical properties |  | Trans. specific resistance | 1 – 100 µΩ.m
 |  | Critical current | (strand props)
 |  | Index of transition | 1 – 1000
Operating conditions |  | Ramp rate of external magnetic field | 0.01 – 1 T/s
 |  | Field orientation | 0 – 90 deg
 |  | Operating current | 0 to Ic
Find current distribution by solving:
Kirchhoff current law for each node (yellow points)
Kirchhoff voltage law for each elementary circuit
Conservation of total operating current
Specified boundary conditions:
:
Dirichlet type: fixed input/output currents (i.e. ‘insulated’ strands outside the modeling region)
Neumann type: fixed current derivatives (zero derivatives  equipotential ends, i.e. short-circuited strands)
Periodic type: account for symmetry in current distribution (suitable to model infinitely long transposed strands) 
https://doi.org/10.1016/j.cryogenics.2018.10.003

## Slide 8: Network modelling: setup and benchmark
The model is validated wrt analytical solutions.
Length = 1 twist-pitch
:
Length = 1 twist-pitch / N
Using periodic BC, –long segment is sufficient for fast analysis w/o accuracy loss.
input currents deduced from the last band
output currents deduced from the first band
first band
last band
x
Full distribution can be obtained as well
Note: intra-strand loss neglected

## Slide 9: Network modelling: power loss
Study on twist-pitch:
Study on critical twist-pitch:
Power loss at the critical value of twist-pitch ~ 50-70% of the saturated loss
Longitudinal
slab estimate
defined from model
analytical
Total
R crossing
R adjacent
saturated loss
slab
Rutherford
slab
Rutherford
model
Typically, n~10-20 for fusion conductors, thus its impact on some 20 – 30%
slab | Rutherford
slab | Rutherford
scaling: less strands -> higher -> lower P inter-strand, but higher P intra-strand

## Slide 10: Network modelling: energy loss
Typical AC loss cycles studied at zero transport current.
However, changing of both transport current and produced magnetic field should be analyzed for actual coil operation 
(weak excitation)
(saturation)
(screening)
Mode |  | 
 | Weak excitation: | Saturation:
 | Screening: | 
Mode |  | 
Time constant:
(weak excitation)
* I/Ic for other strands are similar but phase-shifted

## Slide 11: DEMO CS graded coils: quick overview
https://idm.euro-fusion.org/?uid=2M4P9J
Target: 60 kA / 18 T / 5 K, pulsed operation
R&D on HTS conductors for DEMO CS started this year: 4 concepts by SPC, ENEA and KIT; performance demonstration before 2024
Operating cycle in pulsed tokamaks: advanced 18 T CS graded coils allow increasing burn time, thus higher plant availability by ~10-20% compared to 12 T baseline option.
Coils operated independently, but detailed scenario not yet specified.
https://dx.doi.org/10.5445/IR/1000095873
Assuming 15 T sweep for RU:
Bdot | RU | Flat-top | RD
MIRA | 0.1 T/s | 0.004 T/s | 0.1 T/s
PROCESS | 0.5 T/s | 0.003 T/s | 0.6 T/s
Baseline 12 T DEMO CS:

## Slide 12: DEMO CS graded coils: power loss estimates
CS module | CS3L | CS2L | CS1 | CS2U | CS3U
Most demanding operating conditions | PREMAG: 14.66 T / 70.1o | EOF: 12.59 T / 70.1o | PREMAG: 18.14 T / 83.7o | EOF: 13.16 T / 70.3o | PREMAG: 15.03 T / 70.2o
# of 3.3 mm tapes (aligned along z-axis) | ~220 | ~200 | ~140 | ~200 | ~220
P max for L ~ 1 m | ≈ 2.2 W/m | ≈ 1.7 W/m | ≈ 1.1 W/m | ≈ 1.9 W/m | ≈ 2.4 W/m
P max for L >> 1 m | ≈ 110 W/m | ≈ 80 W/m | ≈ 60 W/m | ≈ 90 W/m | ≈ 120 W/m
Operating current during the cycle
For non-transposed strands, ~100 W/m applied to strands may increase their temperature above 10 K, thus need for higher Tcs.
Strands transposition may reduce losses by about 10 times.
Intra-strand loss should be accounted…
Intra-strand loss is negligible
2.4 W/m + intra-strand loss = 10–20 W/m?

## Slide 13: Outlook on network modelling
DEMO R&W cable
Cable splices
HTS stacked tapes strand
DEMO R&W sub-cable
ASTRA conductor

## Slide 14: Conclusion
THANK YOU FOR YOUR ATTENTION!
Analytical and numerical models are developed to analyze saturated coupling loss in Rutherford cables.
Relatively low loss is obtained by keeping twist-pitch below its critical value expressed as .
Transposition of strands is needed to avoid their overheating during fast transients in the DEMO CS coils.
Network modelling approach is being used to simulate electromagnetic behavior of various cable layouts.