## Slide 1: High Field-Rate Losses in Cable-In-Conduit-Conductors Carrying Transport Current
14th CHATS on Applied Superconductivity (CHATS-AS)
20th-24th September 2021
Virtual (St. Paul Lez Durance, France)
Analytical and Numerical Studies
Gianluca De Marzi, ENEA FSN-COND

## Slide 2: Acknowledgments
University of Roma Tre
Massimiliano Corradini
ENEA
Luigi Muzzi, Lorenzo Giannini, Antonio della Corte
University of Bologna
Marco Breschi, Lorenzo Cavallucci
Swiss Plasma Center - EPFL
Davide Uglietti
Politecnico di Torino
Roberto Bonifetto, Andrea Zappatore

## Slide 3: Outline
Introduction: fast transients in Tokamaks
New model for the calculation of AC losses due to fast varying fields
  Analytical solution of the Osagawara equation
  Coupling, magnetization, and dynamic resistance
Model application: ac losses of a CS module of a Tokamak device (DTT):
  Evaluated AC losses on central turn at peak field
  Developed 2D FE model with variable nt
Conclusions and future directions

## Slide 4: Introduction – Divertor Tokamak Test @ ENEA
18 TF coils:
Nb3Sn CICC: 42.5 kA – 11.9 T
providing 6.0 T over plasma major radius
6 CS modules (indipendently fed):
Nb3Sn CICC: 31.3 kA – 13.6 T
providing 16.6 Weber magnetic flux for
plasma initiation at breakdown
6 PF coils:
Nb3Sn (PF1 & PF6) CICC: 28.3 kA – 9.1 T
NbTi (PF3 & PF4) CICC: 28.6 kA – 5.3 T
NbTi (PF2 & PF5) CICC: 27.1 kA – 4.2 T
Identical in pairs for full top/down symmetry
2.19 m
5.3 m

## Slide 5: High Field-Rates in CS Modules
Premag (t = 0 s)
CS1U
|| during breakdown:
9.7 T/s (CS1U, HF)
7.3 T/s (CS1U, MF)
4.3 T/s (CS1U, LF)
~9.7 T/s
breakdown
Single Null
Peak field, central turns

## Slide 6: Aim of the Work
Allocated thermal budget in SC magnet design
Need to estimate e.m. losses deriving from and/or
2.19 m
5.3 m
The present work investigates the ac losses of conductors subjected to time-varying fields and carrying dc currents.

## Slide 7: Coupling and Eddy Currents in Composites
1970s - Problem studied by several investigators [Morgan, Ries, Carr, Brandt, Clem, Murphy, Norris, etc.]
Solved for trapezoidal shaped Be(t), for two limiting cases:
1978-79 - Extension to higher field-rates attempted by Soubeyrand&Turck
1980 - Ogasawara et al.: saturation layer 𝛿 depends on , and Ries formula no longer valid
D

## Slide 8: Solution of the Ogasawara Problem
Differential equation slightly modified to include both ramp-up and ramp-down
The solution is an implicit function of B
Good news! The solution is integrable, allowing analytical calculations of AC losses
ΔB = 2 T
t0 = 0.25 s
τ = 150 ms
Ic = 1 kA
d = 20 µm
D = 0.82 mm

## Slide 9: Coupling Magnetization
Magnetization per unit volume, Mc, due to the coupling currents
Ogasawara 1980 De Marzi & Corradini 2021
Case (1)
Case (2)
Case (1)
Case (2)

## Slide 10: Coupling Losses
Coupling losses per unit volume Qc: analytical solution for ramping-up field
Ogasawara 1980 De Marzi & Corradini 2021
Case (1)
Case (2)
Case (1)
Case (2)
Case (1)
Case (2)

## Slide 11: Intrinsic Magnetization of SC Filaments
Intrinsic magnetization per unit volume, Mh, due to the shielding currents
Ogasawara 1980 De Marzi & Corradini 2021
Case (1)
Case (2)
Case (1)
Case (2)

## Slide 12: Magnetization Losses
Magnetization losses per unit volume Qh: analytical solution for ramping-up field
Ogasawara 1980 De Marzi & Corradini 2021
Case (1)
Case (2)
Case (1)
Case (2)
Case (1)
Case (2)

## Slide 13: Dynamic Resistance
Resistive voltage per unit length, Vt, due to dynamic resistance
Ogasawara 1980 De Marzi & Corradini 2021
Case (1)
Case (2)
Case (1)
Case (2)

## Slide 14: Losses due to Dynamic Resistance
Dynamic resistance losses per unit volume Qd: analytical solution for ramping-up field
Ogasawara 1980 De Marzi & Corradini 2021
Case (1)
Case (2)
Case (1)
Case (2)
Case (1)
Case (2)

## Slide 15: From Wires to Cables
Can this model be applied to CICCs and coils?

## Slide 16: AC Losses in CS1U, HF Module
328.3
120.8
HF
MF
LF
88.7
105.0
AC losses evaluated considering the
peak field on central turn
τ = 150 ms
Bp = µ0 JCD/2
d = 15 µm
D = 0.82 mm

## Slide 17: AC Losses in CS1U_HF – JC Parameterization
JC parameterization
ITER-2008 with εeff = -0.55%
τ = 150 ms
Bp = µ0 JCD/2
d = 15 µm
D = 0.82 mm
Coefficient | Value
C0 [A T] | 20918
Ca1 | 44.48
Ca2 | 0.0
ε0,a [%] | 0.256
εm [%] | -0.049
Bc2,m(0) [T] | 32.97
Tc0,m [K] | 16.06
p | 0.63
q | 2.1

## Slide 18: Comparative Analysis of AC Losses Results
τ = 150 ms
Bp = µ0 JCD/2
d = 15 µm
D = 0.82 mm
Estimations using standard formulae lead to largely different values
Coupling&magnetization
AC losses tend to top-off to a maximum value  (1-i2)
Decrease of coupling ( -46%) and magnetization ( -9%) losses
Dynamic resistance
At high tB, a dynamic resistance appears against the transport current flow, causing a large increase in AC loss ~ i2: +400%!
Comparison of the results obtained with different models for ac losses
Losses | Units | New formulation | Standard approach | Percentage change [%]
Coupling | [J/m] | 739.4 | 1357.2 | -45.5
Hysteresis | [J/m] | 78.3 | 85.8 | -8.7
Dynamic | [J/m] | 1.85 | 0.36 | 414
Total loss | [J/m] | 819.6 | 1443.4 | -43.2
Total loss | [W] | 737.7 | 1299.1 | -43.2

## Slide 19: AC Losses in CS1U_HF During Breakdown
During breakdown, where tB peaks at 9.7 T/s, full saturation of strands occurs
The strands behave like a solid conductor and a saturation effect takes place in both the magnetization and the ac losses.

## Slide 20: AC Losses in CS1U_HF During Breakdown
During breakdown, where tB peaks at 9.7 T/s, full saturation of strands occurs
The strands behave like a solid conductor and a saturation effect takes place in both the magnetization and the ac losses.
Losses | Units | Whole scenario | During breakdown | Contribution [%]
Coupling | [J/m] | 739.4 | 15.5 | 2.1
Hysteresis | [J/m] | 78.3 | 0.016 | 0.02
Dynamic | [J/m] | 1.85 | 1.4 | 75.7
Total loss | [J/m] | 819.6 | 17.0 | 2.1
Total loss | [W] | 737.7 | 15.3 | 2.1

## Slide 21: Field-Rate Dependent nt in CICCs
In multistage CICCs there exist multiple induced currents loops with a broad range of time constants, affecting different volume fraction of the cable conductors
Bruzzone et al., IEEE TAS 16, 827 (2006); Bruzzone et al., FED 146, 928 (2019)
Depending on the frequency, a dominant time constant can be picked up
  During plasma initiation, the nτ of the CICC approaches the range of the free standing strands
  Lower field changes (i.e., coil charge) are associated with higher nτ values
A single, but field-rate dependent coupling time constant, nt(tB), has been introduced in AC loss models

## Slide 22: Experimental Assessment of nt(tB)
DEMO CICC
DTT-CS CICC
Courtesy of Luigi Muzzi
DEMO WR2 vs. CS-DTT-HF
Similar layouts (rectangular, long twist pitch, low void fraction, SS wrapping)
Different number of SC strands
Sample being inserted for heat treatment
L. Muzzi et al., IEE TAS 31, 4201607 (2021)
M. Kumar, MAG-4.2-T011-D003
The behavior of nt vs. tB is based on the experimental results ​​from recent SULTAN tests on the DEMO Low Field conductor (“WR2”), in which trapezoidal field pulses have been employed
For the procedure to obtain ntpulse, please refer to P. Bruzzone et al., FED 146, 928 (2019)

## Slide 23: FEM Analysis Using Commercial Software
Two-step procedure:
Evaluation of the external field map
  2D axisymmetric FE model
  Magnetic Field (mf) interface, AC/DC Module)
  Coil feature: homogeneized multiturn conductors
Evaluation of AC loss contributions
  Coeff Form PDE interface, Math module
  Time-dependent Bi map
  Calculation of Qc, Qh, Qd (surface averages)

## Slide 24: Recap: AC Losses in CS1U Module, HF Sub-Module
Losses | nt = 0.15 s |  |  | nt=f(tB)
 | Ries | 1 turn | FEM | FEM
Coupling [J/m] | 1357.2 | 739.4 | 584.5 | 639.9
Hysteresis [J/m] | 88.7 | 78.3 | 76.9 | 73.6
Dynamic [J/m] | 0.72 | 1.85 | 4.52 | 0.41
Total loss [J/m] | 1446.6 | 819.6 | 665.9 | 713.9
Total loss [W] | 1302.1 | 737.7 | 599.4 | 642.6
Plasma initiation
(breakdown)

## Slide 25: Future Directions
The qualification phase of the DTT CICC procurements will provide the information for the final choice of the 7 cable layouts
Twist pitch cabling sequence; e.m. cyclic loading; eeff
Coupling time constant nt
Pressure drop, MQE tests and Tcs
The outcome will constitute a test bed for model validation
Analytical model - Unipolar trapezoidal pulses (DB = 0.3 T; t0 = 0.1 to 4 s)
Numerical model - Sinusoidal pulsing (128 ms, 600 V max)
TF Sample manufacturing scheduled Nov. 2021
Courtesy of M. Breschi and L. Cavallucci
AC loss model as input tool for thermo-hydraulic analyses (PoliTo)
THELMA numerical model based on s[S/m2] between cable elements - on going activity (UniBo)
420/180
180/216
162/324
324/162
810/0
300/159
180/213

## Slide 26: Conclusion
Proposed a novel model for the calculation of AC losses due to fast varying fields
  Analytical solution of the Osagawara equation
  Coupling, magnetization, and dynamic resistance
Model applied to a Central Solenoid module of a Tokamak device (DTT):
  Evaluated AC losses on central turn at peak field
  Developed 2D FE model with variable nt
Future directions: model validation
  SULTAN tests with trapezoidal ramps
  Benchmark with other approaches (UniBo)
  Other off-normal scenario still to be analyzed, with special reference to quench and disruptions

## Slide 27
Gianluca De Marzi
gianluca.demarzi@enea.it