## Slide 1: Tungsten sputtering due to fast particles in ITER
A. Snicker et al.

## Slide 2: A. Snicker, K. Särkimäki, S. Saari, L. Aho-Mantila – VTT Technical Research Centre of Finland Ltd. Espoo, Finland T. Kurki-Suonio, A. Sand – Aalto University, Espoo, Finland M. Garcia-Munoz – University of Seville, Seville, Spain K. Schmid - IPP Garching, Germany S. Wiesen – DIFFER, The Netherlands S. Henderson, K. McClements – UKAEA, United Kingdom H. Kumpulainen - Forschungszentrum Jülich, Germany

## Slide 3: Fast ions pose a risk to the plasma and the first wall
Poor fast ion confinement:
  Loss of heating -> degraded performance
  Losses of fast ions

## Slide 4: Fast ions can pose risk to the plasma and the first wall
Bad fast ion confinement will result in:
  Loss of heating -> degraded performance
  Losses of fast ions
Fast ion losses can:
  Directly endanger the wall -> damage PFCs
  Indirectly degrade plasma performance by sputtering impurities
J. Galdon-Quiroga et al 2018 Nucl. Fusion 58 036005

## Slide 5: Fast ions can pose risk to the plasma and the first wall
Bad fast ion confinement will result in:
  Loss of heating -> degraded performance
  Losses of fast ions
Fast ion losses can:
  Directly endanger the wall -> damage PFCs
  Indirectly degrade plasma performance by sputtering impurities
J. Galdon-Quiroga et al 2018 Nucl. Fusion 58 036005
H. Sheng et al 2026 Nucl. Fusion 66 036023

## Slide 6: Fast ions can pose risk to the plasma and the first wall
Bad fast ion confinement will result in:
  Loss of heating -> degraded performance
  Losses of fast ions
Fast ion losses can:
  Directly endanger the wall -> damage PFCs
  Indirectly degrade plasma performance by sputtering impurities
In this talk: Numerical assessment of W sputtering due to fast particles in ITER
J. Galdon-Quiroga et al 2018 Nucl. Fusion 58 036005
H. Sheng et al 2026 Nucl. Fusion 66 036023

## Slide 7: What is needed for the assessment?
Database of fast particle losses

## Slide 8: What is needed for the assessment?
Database of fast particle losses
  NBI and alpha particles losses
T Kurki-Suonio et al 2017 Plasma Phys. Control. Fusion 59 014013

## Slide 9: What is needed for the assessment?
Database of fast particle losses
  NBI and alpha particles losses
  CX losses of NBI and alpha particles -> this talk!
T Kurki-Suonio et al 2017 Plasma Phys. Control. Fusion 59 014013

## Slide 10: What is needed for the assessment?
Database of fast particle losses
  NBI and alpha particles losses
  CX losses of NBI and alpha particles
T Kurki-Suonio et al 2017 Plasma Phys. Control. Fusion 59 014013
Sputtering yields for D and He
  Correct energy range and resolution -> this talk!
Figure by K. Schmid

## Slide 11: What is needed for the assessment?
Database of fast particle losses
T Kurki-Suonio et al 2017 Plasma Phys. Control. Fusion 59 014013
Sputtering yields for D and He
Figure by K. Schmid
A workflow to estimate sputtered W
  Here: ASCOT5 + SDTrimSP 7.0 + python script

## Slide 12: Outline Introduction Sputtering yield data CX model in ASCOT5 Analysis on ITER alpha particles Conclusions and future work

## Slide 13: Sputtering data for fast particles
Sputtering yields function of incoming particle energy and incidence angle
  Higher the energy, lower the yield
  More normal (=0 degrees) incidence angle, lower yield
Standard way to obtain sputtering data is by simulations
  Here, SDTrimSP 7.0 will be used
Yield data is needed in 2D grid, with suitable resolution
Towards high E, calculations are expensive
Perform high resolution map for D and He ->
4He, D

## Slide 14: Sputtering yields as a function of energy
Note: He decays slower than D

## Slide 15: Sputtering yields as a function of incident angle

## Slide 16: Impact of refined sputtering yield to W sputtering
With scarce yield and poor interpolation
  ITER W total source: 8.45e+16 W/s
With extensive yield data and refined interpolation
  ITER W total source 7.55e+16 W/s
Difference (Δ=-8.97e15 W/s, -10.6%)
Sputtering yields and interpolation ready for production
  To be shared with the publication following this contribution

## Slide 17: Outline Introduction Sputtering yield data CX model in ASCOT5 Analysis on ITER alpha particles Conclusions and future work

## Slide 18: Fast particles can charge exchange with neutrals
Typically implemented for H, D
  Re-ionization using effective cross-section (BMS)
CX cross-section data from ADAS
Suitable for NBI particles in ITER
What about the alphas?
P. Ollus. Modelling charge exchange losses of beam ions in the MAST-U spherical tokamak. Master’s thesis, Aalto University, 2019. Available at: https://urn.fi/URN:NBN:fi:aalto-201912226660.

## Slide 19: Sputtering due to CX – case alphas
Do not assume Z=1
  Need to track charge state
After 1st CX alpha can:
  Undergo 2nd CX
  Re-ionize
Using BMS not possible
  Consider individual reactions

## Slide 20: Details of ASCOT5 CX implementation
Open-ADAS only provides data for BMS
Instead of relying on ADAS, IAEA ALADDIN was used.
  Both CX reactions from C.F. Barnett, ORNL-6086, 1990.
  Electron-impact ionization from Janev, H-He Plasma, 1987
  Ion-impact ionization potentially significant but not (yet) included
Testing the implementation by mock-up cross-sections

## Slide 21: Outline Introduction Sputtering yield data CX model in ASCOT5 Analysis on ITER alpha particles Conclusions and future work

## Slide 22: Numerical assessment for 15MA H-mode ITER scenario
Standard 3D magnetic field
  TF ripple, FIs, TBMs, ECCs+plasma response
Store locations of wall hits, incidence angle and energy
Interpolate sputtering yields from 2D grids
Integrate total sputtering source rates
Goal: 1st order estimate on fast particle induced sputtering
  Comparison against other sources of W
[Jari Varje et al 2016 Nucl. Fusion 56 046014]

## Slide 23: Alphas lost with large incidence angles
Divertor
Outer midplane

## Slide 24: Alpha source (to wall) -> W source (from wall)
x sputtering yield

## Slide 25: Alpha induced W source vs. WallDyn sources in ITER
“Assume a pure W wall exposed to 100% recycling species: D, D-CX, Ne and partially recycling W”
Figures: S. Weisen, H. Kumpulainen

## Slide 26: Alpha induced W source vs. WallDyn sources in ITER
Figures: S. Weisen, H. Kumpulainen
Other sources 5e20 vs. alpha induced 2e16 W/s!

## Slide 27: Outline Introduction Sputtering yield data CX model in ASCOT5 Analysis on ITER alpha particles NBI and CX alphas Conclusions and future work

## Slide 28: Charged NBI sputtering
NBI losses ~ alpha losses
T Kurki-Suonio et al 2017 Plasma Phys. Control. Fusion 59 014013
Sputtering yield for D < for He
Figure by K. Schmid
Sputtering due to NBI ~ due to alphas
Charged NBI sputtering can be ignored!

## Slide 29: Contributions from CX losses (preliminary results)
Neutral 1D density from JINTRAC
Nonimal SOL value 1e13 m-3
Scale SOL value up to 1e17 m-3
CX significant only at 1e17 m-3 density
Caveats:
  Neutral density is highly 2D/3D
  Neutral density poorly estimated
Consider results as 1st order estimate
Species | n0=0 | n0=1e13 | n0=1e17
NBI | 1.6 MW | 1.6 MW | 2.3 MW
Alpha | 1.1 MW | 1.1 MW | 1.6 MW

## Slide 30: Outline Introduction Sputtering yield data CX model in ASCOT5 Analysis on ITER alpha particles NBI and CX alphas Conclusions and future work

## Slide 31: Fast particle induced W sputtering in ITER
Charged alpha particle lost induced W source < other W sources
Charged NBI induced W source comparable to alpha source
CX lost source only significant at large neutral density at SOL
Within these assumptions, fast particle induced W source can be ignored in ITER

## Slide 32: Was it worth it? Lessons learned and side products
Obtained fast particle relevant sputtering yields for D->W and He->W
  Usable for any device, with potentially different geometry
Generalized CX model usable for alpha induced CX
  Depending on neutral, ion and electron density, alpha CX can be important
From SDTrimSP, we obtain reflection coefficients
  Could be used to finetune fast particle wall power load estimates ->

## Slide 33: Reflection coefficients for alphas and NBI particles
SDTrimSP gives a reflection co-efficient
The coefficient is well above zero for both He and D

## Slide 34: Main caveats and question marks
Are the SDTrimSP 7.0 simulations accurate
  Experimental validation challenging
Are we comparing against reliable “other W sources”?
For CX, neutral density should be 2D/3D
Likely modify results quantitatively but not qualitatively

## Slide 35
A. Snicker